|  | STANDARDS ASSOCIATION OF ZIMBABWE |
| --- | --- |

DRAFT FOR PUBLLIC COMMENTS

LATEST DATE FOR RECEIPT OF COMMENTS: 2025-10-24

Our ref: BC 048 – FDZWS 233:2025 Draft Number FDZWS 233: 2025 Date: 2025-08-28

TECHNICAL COMMITTEE BC 048: CONCRETE - REINFORCED CONCRETE AND PRE-STRESSED CONCRETE

-----------------------------------------------------------------------------------------------------

ZIMBABWE STANDARD SPECIFICATION FOR AGGREGATES FROM NATURAL SOURCES FOR CONCRETE

This draft is now available for public comment. Your views and technical comments on it would be appreciated.  If you have no specific comments to make but find it generally acceptable it would be helpful if you would notify us accordingly. Suggestions entailing revisions of the text should indicate the preferred wording using the attached template.  The relevant clause number should be quoted against any comment.

All comments should be sent to the Committee Secretary E.Pindura at the address shown below.

Standards Association of Zimbabwe

P O Box 2259

Harare

E-mail: epindura@saz.org.zw

THIS IS A DRAFT AND MUST NOT BE REGARDED OR USED AS A ZIMBABWE STANDARD.

Copyright Users of Zimbabwe National Standards are reminded that copyright subsists in all ZWS publications. No part of this publication may be produced in any form or by any means, electronic or mechanical, including photocopying or posting on the internet or an intranet, without prior permission in writing from the Director General of the Standards Association of Zimbabwe. Orders for all national, international and foreign standards publications should be addressed to: Director – Standards Development, Information and Training Standards Association of Zimbabwe P O Box 2259 Harare Northridge Park Borrowdale Tel: 885511-2, 882017-9, 882021-2 Fax: 882020 E-mail: info@saz.org.zw Website: www.saz.org.zw

Contents											Page

Foreword 			iv

- Scope		 	1

2.	Definitions  	   	1

3.	Quality Of Aggregates 		1

4.	Sampling And Testing 	 	4

- Additional Information  		5

6.	Marking Of Deliveries 		5

Appendix A – Notes on The Interpretation of Test Results		6

Appendix B – Petrographic Overview		12

Appendix C – General Interpretation of Petrographic Examination 		13

Appendix D – Recommended Proportion for Blending Aggregates 		15

Foreword

This Zimbabwe Standard ZWS 233:2025: Aggregates from natural sources for concrete, is the third revision of ZWS 233:1997. The standard was revised to bring it in line with the latest technology in the building industry.

This standard was revised by technical committee BC 048: Concrete - Reinforced Concrete and Pre-Stressed Concrete, which falls under the Building and Civil Engineering Standards Sector.

First published 1969, as CAS A34,

First revision 1978, as CAS A34,

First reprint 1978, as ZWS 233,

Second revision 1997, as ZWS 233,

First reprint 2004, as ZWS 233,

Third revision 2025, as ZWS 233.

This standard makes reference to the following publications:

ASTM C 289	:	Test method for potential reactivity of aggregates (Chemical method).

ZWS EN 12350	:	Testing fresh concrete

Part 1	:	Sampling

Part 2	: 	Slump test

ZWS EN 12390	:	Testing hardened concrete

Part 1	:	Shape, dimensions and other requirements for specimens and moulds

Part 2	:	Making and curing specimens for strength tests

Part 3 	:	Compressive strength of test specimens

Part 7	:	Density of hardened concrete

ZWS 185	:	Methods of testing soils for civil engineering purposes.

Part 1	:	Preparation, classification and density of soils.

ZWS 190	:	Methods for sampling and testing of aggregates and fillers.

ZIMBABWE STANDARD SPECIFICATION

FOR

AGGREGATES FROM NATURAL SOURCES FOR CONCRETE

(Third Revision of ZWS 233:1997)

1.	Scope

This Zimbabwe Standard covers naturally occurring materials for use in the production of normal structural concrete. The materials may have been produced by crushing, washing and/or screening or other processes to ensure compliance with the requirements of this standard.

Note. The titles of the publications referred to in this standard are listed in the Foreword.

2.	Definitions

For the purpose of this Zimbabwe Standard the following definitions shall apply: